Assignment 4

Match the words in bold to the types of signaling: repetition, summary word, connector.

| Repetition | Summary word | Connector |
| --- | --- | --- |
| AI-Mg-Si alloys | … | … |
| … | … | … |
| … | … | … |

The heat treatment strengthening Al-Mg-Si alloys have been widely used in the automobile vehicles and marine structure due to their desirable combination of high strength and moderate corrosion resistance. It has been generally accepted that the main precipitation sequence of Al-Mg-Si alloys during artificial aging treatment is: SSSS (super-saturated solid solution) → GP zones→β″ → β′,U1,U2 → β [1][2][38]. The β″ phase is widely accepted to be the most strengthening phase within the aluminum matrix of Al-Mg-Si alloys.

Recently, trace alloying element Sn has been used for preventing detrimental effect of natural aging on the mechanical properties of Mg-rich alloys, such as AA6061 alloy [3].  Such additive can trap the vacancy during the quenching process and therefore restrain the process forming MgSi clusters at room temperature, which results in irreversibly detrimental impact to strengthening ability of Al-Mg-Si alloys. Besides, the effectiveness of  Sn addition to retard natural aging hinges on the maximum solubility of Sn in Al matrix, because excess Sn not in solid solution tend to form intermetallic compound so that they cannot further trap vacancy. According to the phase diagram, Sn has very little solubility in aluminum (i.e. 0.1 wt% at ~600 °C). Approximately 0.044 wt% Sn can be dissolved in Al-Mg-Si alloy AA6061 when it is solution treated at 570 °C. The strong binding effect between Sn and vacancy becomes weak at higher temperature (~180 °C). Those  Al-Mg-Si alloys with Sn addition can achieve much higher peak hardness when aged at 210–250 °C [4][5], but it is still unclear that whether various Sn contents would have influence on the mechanical properties of Al-Mg-Si alloys when the alloys are aged at relatively lower temperature (~170 °C). There were investigations focused on the mechanical effect of Sn addition on 2xxx alloys and 7xxx alloys [6][23][34][36]. Compared to the Sn-free alloys, those alloys containing certain trace Sn have higher ultimate tensile strength (UTS) and yield strength (YS) after artificial aging. The Sn-added alloy can achieve better performance by refining the precipitate or reducing the width of PFZ along the grain boundary.

In Al-related battery filed, investigations focused on ameliorating the performance of the Al-air battery proposed that Sn can effectively reduce the parasitic corrosion and activate the aluminum by breaking down the passive hydroxide layer [8][9][13][37]. Consequently, appropriate Sn addition can accelerate dissolution of Al. An investigation concerning Al-Mg-Sn-Ga alloy anodes suggested that compared to those Sn elements that present as precipitates, Sn elements in solid solution can effectively reduce the corrosion rate and hydrogen release [10]. It has been suggested that those Sn particles in solid solution tend to accelerate anodic dissolution of aluminum, according to a report that the resistance of the surface oxide film, which prevent the metal from corrosion, reduces to tiny value [11]. Another investigation showed that the Sn addition in solid solution with aluminum (i.e. 0.02 wt%) exhibited almost the same corrosion morphology as aluminum did. A higher level of Sn content (i.e. 0.4 wt%) can result in much higher anodic dissolution, which gives rise to severe corrosion attack [11][13]. In summary, appropriate Sn addition (in solid solution with Al) may moderately accelerate the dissolution of Al but not at fast rate. It has been investigated that the composition of the alloy must be chosen in order to ensure the complete solution of Sn within the aluminum matrix and no formation of other Sn-related phase such as Mg2Sn phase or Sn particles [12][16]. That is to say, when the concentration of Sn addition transcends its solubility at certain heat-treatment temperature, those excess Sn tends to precipitate at the grain boundary and serve as the ‘active’ centers compared to the surrounding aluminum matrix. Thus, the anodic dissolution happens and there is pitting corrosion around the Sn-related precipitates. Study on the corrosion behaviors of Al-Mg-Si alloys showed that Mg2Si phase exhibit an open circuit potential of ~1.2 VSCE, which is relatively active as opposed to the Al matrix [14]. An article demonstrated that the open circuit potentials of PFZ is negative than that of the matrix [15], which can act as an anodic site during corrosion process. In addition, Mg2Sn phase possess higher potential than that of the Al matrix. Pitting Corrosion is able to happen around the Mg2Sn phase with the dissolution of Al [16].